## Slide 1
ACARP PROJECT C17004 UPDATE:
TOUGH SKIN – A SPRAY-ON POLYMERIC REPLACEMENT FOR ROOF & RIB MESH
Chris Lukey, Ernest Baafi, Jan Nemcik, Ian Porter
School of Civil, Mining & Environmental Engineering
Faculty of Engineering
University of Wollongong
Roadway Development Operators’ Workshops
August/September 2009
Notes: <number>

## Slide 2
Objectives
To develop an alternative to steel mesh that:
Provides an effective skin confinement measure equivalent or superior to that of steel mesh
Requires minimal human intervention in its installation
Removes personnel from the immediate face area
Enables higher underground roadway development rates to be achieved
Is safe to use
Is cost effective
The focus of our work is the development of a polymer-based alternative that can be spray-applied
Notes: <number>

## Slide 3
Progress Since March 2009
Shelf Life issues resolved
Surface temperature measurement during cure
Comparison of reinforcements
- short and long glass fibre
- short carbon fibre
Study of alternative flame retardants
- progress but limited success
Wind tunnel second experiments
Handling of reinforcement during spray
Commenced accelerated performance tests
Commenced study of intercoat adhesion
Commenced study of effect on downstream processing
Notes: <number>

## Slide 4
Surface Temperature Measurements
Notes: <number>

## Slide 5
Flexure Test Comparison
of Long and Short Glass Fibre Reinforcement
Notes: <number>

## Slide 6
Two types of tests in two different-sized wind tunnels:
Static tests (small and large tunnel)
Spray tests (large tunnel only)
Conducted with minimum permissible air velocity (0.5m/s) to simulate
worst-case mine ventilation scenario
Surface temperature monitored during cure
Air samples collected upstream and downstream in large tunnel:
* During spray/cure
* Immediately after spray/cure
* After one further hour whilst maintaining ventilation in the tunnel
No reinforcement included
Wind Tunnel Tests
Notes: <number>

## Slide 7
Fan
Air “Straightener”
Large Wind Tunnel Redesigned
Flow Direction
Notes: <number>

## Slide 8
Spray Duration
Ambient Temperature 16.5°C
Surface Temperature During Spray
Notes: <number>

## Slide 9
Conceptual Design of Feed System
for Spraying of Reinforcement
Notes: <number>

## Slide 10
Future Work
Accelerated performance tests:
Measure effect on mechanical properties of
- water at ambient temperature
- water at elevated temperatures
- water at different pH
- elevated temperatures
Intercoat adhesion:
Does fresh material stick to already-cured material?
- encouraging early results
Effect of “Tough Skin” on downstream processing:
- student project
- encouraging early results
Study of alternative flame retardants & anti-stats:
- testing at MSTC (Hunter Valley)
Notes: <number>